everything

for the repair and

preservation of wood

and plastic surfaces

... from König

König Sprays

Technical Leaflet	Prime Lacquer White  Kö 359

Uses:

	A strongly embeding, completely covering primer if interior parts, medium tight fibre-boards and chipboards

are to be coated by Covering Lacquer afterwards.

	A mobile spray system for priming work.

Properties:

	White-dyed primer based on nitrocellulose. Physically drying system.

	Good integration and running properties with excellent hardness and resistance.

	Very good for sanding.

	Not Soft-PVC-resistant.

Processing Advice:

	Shake can well before use.(If ball agitators are not heard while shaking, hold can upside down and try again.)

When banging of ball agitators is audible – shake at least for another 30 seconds. Repeat procedure several

times during work process.

	Process at room temperature – do not spray on cold surfaces.

	In case of horizontal surfaces spray wet coat onto areas that have been ground and freed from dust.

	In case of vertical surfaces several (2-3) coatings - not too wet sprayed - are of advantage.

	Before sanding, at room temperature, let flash off for approx. 30 minutes - depending on the coating's

thickness.  Afterwards grind with Sandpaper dry Kö 414 grain 280-400 and remove dust residues carefully.

	Make a test on an inconspicuous area first.

Professional Hints from the Training Centre:

	In order to avoid a sticky spray nozzle, always work with the black spray nozzle – this ensures an even-

looking surface.

	Take care of flash off-period between individual work processes to be approx. 30 minutes.

	After a drying period of approx. 1 hour - depending on the coating's thickness - final coating with

Covering Lacquer can be done. Carefully free from dust first.

	To attain better spray properties the König Spray can may be warmed up in a hot water bath to max. 50°C

for 1-2 minutes.

	Take care of clean spray nozzle.

Lacquer residues may cause a sticky and blocked spray nozzle. It can be cleaned by putting it onto a

Moisture and Bloom Remover can and 'sprayed clean'.

Available:	König Spray 150 ml/400 ml

1st issue 03/98		page 1 of 2

König Sprays

Prime Lacquer White  Kö 359		Technical Leaflet

Tests:

	Drying period

According to the ground underneath and the amount sprayed, at room temperature, after 15-20 minutes

dust dry, after 30 minutes to be ground.

	To be used on the following grounds

Genuine wood, genuine wood veneer, chipboards, plywood and medium tight fibre-boards.

	To be lacquered over with other König lacquers

To be lacquered over with any product of the König-range.

	Richness

The contents of a 400 ml can lasts for approx. 1,0 sqm (single treatment). Richness depends on the

absorptive capacity of the ground underneath.

Safety Advice:

	Extremely flammable.

	Pressurized container.

	Protect from sunlight and do not expose to temperatures exceeding 50°C.

	Do not pierce or burn, even after use.

	Do not spray on a naked flame or any incandescent material.

	Keep away from sources of ignition. – No smoking.

	Keep out of the reach from children.

Information on Safe Use:

	Subject to the Dangerous Substances Regulations of Germany. For further information please refer to our

Material Safety Data Sheet.

	Without adequate ventilation formation of explosive mixtures may be possible.

	Do not spray into eyes.

	Do not breathe vapour.

Disposal Information:

	Dispose of König Spray cans only when completely emptied according to the official rules. Please refer to

the Material Safety Data Sheet or ask your local waste industry office.

	Heinrich König & Co. takes care of the disposal of König Spray cans provided they are returned carriage

paid to the address stated below.

This information is given to the best of our knowledge, is supposed to and can only give advice without guarantee.

If applicable in isolated cases procedure specifications have to be adjusted to special requirements.

Heinrich König & Co.    An der Rosenhelle 5    61138 Niederdorfelden    Germany

Tel. 06101 - 53 60 0    Fax 06101 - 53 60 11

Page 2 of 2